## Slide 1
Ohira et al.
Ultrahigh pressure structural changes in a 60 mol. % Al2O3–40 mol. % SiO2 glass
Ohira et al. (2019) Geochem. Persp. Let. 10, 41-45 | doi: 10.7185/geochemlet.1913
© 2019 The Authors
Published by the European Association of Geochemistry
under Creative Commons License CC BY-NC-ND.
Figure 2 The first (r1), second (r2), and third (r3) peak positions of g(r) of the A40S glass. (a) Red, blue, and black circles indicate the r1 determined in the high pressure experiments 1 and 2, and at ambient pressure, respectively. Triangles indicate the Si–O bond distance in SiO2 glass (Sato and Funamori, 2010). Open diamonds and squares indicate the Si–O and Al–O bond distance in CaAl2Si2O8 glass, respectively, simulated with 416 (black) and 208 (gray) atom simulation cells (Ghosh and Karki, 2018). The black dash lines are obtained from fitting for …
Notes: Figure 2 The first (r1), second (r2), and third (r3) peak positions of g(r) of the A40S glass. (a) Red, blue, and black circles indicate the r1 determined in the high pressure experiments 1 and 2, and at ambient pressure, respectively. Triangles indicate the Si–O bond distance in SiO2 glass (Sato and Funamori, 2010). Open diamonds and squares indicate the Si–O and Al–O bond distance in CaAl2Si2O8 glass, respectively, simulated with 416 (black) and 208 (gray) atom simulation cells (Ghosh and Karki, 2018). The black dash lines are obtained from fitting for the Si–O and Al–O bond distances with CN = ~6. The light blue and orange lines are obtained from fitting the r1 of A40S glass at 35–102 GPa using the drSi–O(6CN)/dP and the drAl–O(6CN)/dP, respectively. The widths of lines indicate the fitting errors. (b) The r2 and r3 of the A40S glass determined in the experiments 1 (red) and 2 (blue), respectively.
Figure 1 (a) Structure factors, S(q), of molten CaCO3; curves are stacked to see better the evolution with increased P-T conditions (given on the right panel); the main change affecting S(q) (Fig. 1a) is the shift of the first sharp diffraction peak (FSDP) towards higher reciprocal distances, up to 2.28 Å-1 at 8.7 GPa which corresponds in the real space to a characteristic mid-range order distance, 2𝜋/𝑞_𝐹𝑆𝐷𝑃, of 2.76 Å. (b) Corresponding radial distribution functions (plain curves), g(r), compared to MD simulations (dashed curve; Vuilleumier et al., 2014).