## Slide 1
Petitgirard et al.
Magma properties at deep Earth’s conditions from electronic structure of silica
Petitgirard et al. (2019) Geochem. Persp. Let. 9, 32-37 | doi: 10.7185/geochemlet.1902
© 2019 The Authors
Published by the European Association of Geochemistry
under Creative Commons License CC BY-NC-ND.
Figure 1 XRS spectra of Si L2,3 and O K-edge up to 110 GPa from experiment and calculations. (a,b) Si L2,3 spectra. (c,d) O K-edge spectra. Grey spectra in a and c show measurements at the starting pressure indicated on the right, the coloured spectra correspond to the final pressure. (e) Atomic structure of SiO2 from MD.
Notes: Figure 1 XRS spectra of Si L2,3 and O K-edge up to 110 GPa from experiment and calculations. (a,b) Si L2,3 spectra. (c,d) O K-edge spectra. Grey spectra in a and c show measurements at the starting pressure indicated on the right, the coloured spectra correspond to the final pressure. (e) Atomic structure of SiO2 from MD.
Figure 1 (a) Structure factors, S(q), of molten CaCO3; curves are stacked to see better the evolution with increased P-T conditions (given on the right panel); the main change affecting S(q) (Fig. 1a) is the shift of the first sharp diffraction peak (FSDP) towards higher reciprocal distances, up to 2.28 Å-1 at 8.7 GPa which corresponds in the real space to a characteristic mid-range order distance, 2𝜋/𝑞_𝐹𝑆𝐷𝑃, of 2.76 Å. (b) Corresponding radial distribution functions (plain curves), g(r), compared to MD simulations (dashed curve; Vuilleumier et al., 2014).